Spray Coater

Chamber Dimension – 94X83X79cm (X,Y,Z)

Chamer is close connected to the exhaust (from baskside) – 90-150 CFM

Work area – 40X40X10cm (X,Y,Z)

Hot plate - ~100c

Viscosity upper limit: 50 cps

Solid concentration upper limit: 40%

Please fill the following Topics:

1.Spray coating parameters:

- Substrate :  10X10cm Freudenberg carbon paper

- Spray material information: Pt and Ir nanoparticles (1%wt solids) in de-ionized water, IPA and Methyl Ethyl Ketone (MEK), with Nafion binder.

- Coating parameters : 100C, target solid load 3mg/cm2. Total ink volume per electrode – 43.2ml

- General information about the process – spray coating of catalytic ink onto carbon paper.

2. MSDS documents: MEK MSDS attached to the email.

3.Safety aspects:

Please specific any hazard and any specials handling requirements:

- proper ventilation is required

- the solution and the deposit is flammable; need to be careful about any nearby ignition sources and oxidizers.

4.Safety precautions:

* keep away from open flame.

5.Disposal:

* leftovers will be collected and disposed by Purammon

*Send this protocol for approvements before first use