Estrales

Choose only 2

Main specifications

- Gases- SF6, C4F8,O2

- 4’’ wafer, 7mm edge clamp

- ER up tp 1.5(um/min) for HAR

- Selectivity- more than 20:1 to PhR, 40:1 to SiO2

- ~Profile 90 deg

- Uniformity - ~5%

- Scallop- 5nm(Cryo)

Requirements-

Bosch process- alternating deposition and etch step, interleaved clean regime (plasma, mechanical )

Feature size- 10um width, AR 1:1, depth<1um, 20% exposed area

Mask sidewall profile- >87%

PhR- AZ45662,S1818…

Mask thickness- 2XEtch depth/selectivity

Calculations:

Etch depth-	* wafer uniformity- max-min2*Avg*100%

* Batch uniformity – maxavg-minavg2*Avg*100%

* Reproducibility (run to run) uniformity – maxavg-minavg2*Avg*100%