Cobra

Choose only 2

Main specifications

- Gases- SF6, C4F8,O2, Ar, N2O, He,Cl2, BCl3, C2H4

- 4’’ wafer, 7mm edge clamp

- ER up tp 20(nm/min) for Sapphire

- Selectivity- more than 2:1 to PhR, 5:1 to Ni

- ~Profile 80 deg

- Uniformity - ~5%

Requirements-

Feature size- 10um width, AR 1:1, depth<1um, 20% exposed area

Mask sidewall profile- >87%

PhR- AZ45662,S1818…

Mask thickness- 2XEtch depth/selectivity

Calculations:

Etch depth-	* wafer uniformity- max-min2*Avg*100%

* Batch uniformity – maxavg-minavg2*Avg*100%

* Reproducibility (run to run) uniformity – maxavg-minavg2*Avg*100%